SIMULATION SPECIFICATION DOCUMENT

For ML/Computational Simulation of Hydrogen Adsorption

in a Zeolite–Nano-AC Composite Physisorption System

| DOCUMENT INFORMATION |  |
| --- | --- |
| Project Title | Design and Testing of a Prototype Physisorption Hydrogen Storage System Using Zeolites and Nano-Activated Carbon Composite |
| Prepared by | Emmanuel Solomon-Eseh ("Snow") |
| Department | Petroleum & Gas Engineering, University of Lagos |
| Drawing Reference | PID-ZHS-FAB-002, Rev C1 |
| Document Purpose | Complete specification for computational/ML simulation handoff |
| Simulation Goal | Full performance comparison across all 8 experimental configurations |
| Date | 22 August 2026 |

# 1. Overview and Context

This document provides the complete technical specification required for a computational or machine-learning-based simulation of hydrogen adsorption in a prototype zeolite–nano-activated carbon composite storage system. The physical prototype is designed around the P&ID drawing PID-ZHS-FAB-002 and operates via a dry-ice and acetone cooling bath at 195 K. Because physical hydrogen gas is unavailable for experimental testing, simulation is adopted as the primary means of generating the performance data required for Chapter 4 of the final year thesis.

The person running the simulation should read this entire document before beginning any computational work. Every parameter, material property, operating condition, and output requirement relevant to the simulation is specified here. Where a range of values is given, the preferred value is indicated. Where assumptions have been made, they are flagged explicitly so the simulator can refine them if better data is available.

## 1.1 What the Simulation Must Reproduce

The simulation must generate adsorption isotherms — that is, the equilibrium quantity of hydrogen adsorbed per unit mass of adsorbent as a function of pressure at a fixed temperature — for eight distinct material configurations at a temperature of 195 K and pressures of 1, 3, 5, 7, and 10 bar. The eight configurations arise from the combination of two zeolite types, two physical forms, and two composite variants defined in the experimental test matrix.

## 1.2 Recommended Simulation Approach

Three simulation approaches are viable for this system, listed in order of preference:

- Grand Canonical Monte Carlo (GCMC) — MOST RECOMMENDED. This is the gold standard for predicting gas adsorption isotherms in porous materials. It directly simulates the statistical equilibrium between a gas-phase reservoir at fixed chemical potential (pressure) and the adsorbed phase inside the zeolite pores. Software: RASPA2 (free, open source). This approach requires zeolite crystal structure files (.cif format) and a hydrogen force field.

- Machine Learning Surrogate Model — SECOND CHOICE. Train a model on published isotherm data from the literature (Langmi 2003, Erdogan 2024, Hauli 2025, Akyalcin 2024) and use it to predict isotherms for the eight configurations. Software: Python (scikit-learn, XGBoost, or a neural network). This approach does not require crystal structure files but requires careful feature engineering.

- Density Functional Theory (DFT) + Statistical Mechanics — THIRD CHOICE. Computationally expensive, requires specialist expertise. Not recommended unless the simulator has specific DFT experience.

NOTE: Regardless of which approach is used, the simulator must validate the output against the published Langmi et al. (2003) values for plain Zeolite 13X and 5A at 77 K before proceeding to generate the 195 K predictions. This is the non-negotiable quality check.

# 2. Material Specifications

This section provides the complete material property data the simulator needs to define the adsorbent phases. Every parameter listed here is required as an input to the simulation.

## 2.1 Zeolite 13X — Primary Adsorbent (Configuration A)

| Property | Value | Source / Notes |
| --- | --- | --- |
| Framework type | Faujasite (FAU) | Standard crystallographic classification |
| Si/Al ratio | 1.0 – 1.5 | Typical commercial 13X; use 1.0 if not specified |
| Extra-framework cation | Na⁺ (sodium) | NaX form, fully exchanged |
| Pore aperture diameter | 7.4 Å | 12-membered ring opening |
| Supercage diameter | 11.8 Å | FAU supercage |
| BET surface area | 700 – 900 m²/g | Target: 800 m²/g for simulation baseline |
| Micropore volume | 0.25 – 0.35 cm³/g | Target: 0.30 cm³/g |
| Crystal density | 1.92 g/cm³ | Pure crystalline phase |
| Pellet bulk density (granular) | ~0.60 g/cm³ | Includes binder phase |
| Binder content (granular form) | 15–20 wt% | Clay or silica binder; use 17.5% if unknown |
| CIF file reference | FAU framework — IZA Structure Database | Download from iza-structure.org |
| Isosteric heat of adsorption (H₂) | 4 – 8 kJ/mol | Use 4 kJ/mol for conservative estimate |
| Langmuir saturation capacity | ~1.5 wt% at 77 K | From Langmi et al. (2003) |

## 2.2 Zeolite 5A — Secondary Adsorbent (Configuration B)

| Property | Value | Source / Notes |
| --- | --- | --- |
| Framework type | Linde Type A (LTA) | Ca-exchanged form (5A) |
| Extra-framework cation | Ca²⁺ / Na⁺ mixed | Ca²⁺ dominant in 5A |
| Pore aperture diameter | 4.2 Å | 8-membered ring opening |
| Alpha-cage diameter | 11.4 Å | LTA alpha cage |
| BET surface area | 600 – 750 m²/g | Target: 680 m²/g |
| Micropore volume | 0.22 – 0.28 cm³/g | Target: 0.25 cm³/g |
| Crystal density | 1.52 g/cm³ | Pure crystalline phase |
| Pellet bulk density (granular) | ~0.70 g/cm³ | Includes binder phase |
| Binder content (granular form) | 15–20 wt% | Same as 13X, clay binder |
| CIF file reference | LTA framework — IZA Structure Database | Download from iza-structure.org |
| Isosteric heat of adsorption (H₂) | 4 – 7 kJ/mol | Use 4 kJ/mol for conservative estimate |
| Langmuir saturation capacity | ~1.0 wt% at 77 K | From Langmi et al. (2003) |

## 2.3 Nano-Activated Carbon — Composite Additive

| Property | Value | Source / Notes |
| --- | --- | --- |
| Particle size | < 100 nm | Nano-grade, not standard activated carbon |
| BET surface area | ≥ 1,000 m²/g | Minimum specification |
| Micropore volume | ≥ 0.40 cm³/g | High-micropore-volume grade |
| Total pore volume | 0.6 – 1.2 cm³/g |  |
| Carbon content | ≥ 95 wt% | Analytical grade |
| True density | 2.0 – 2.2 g/cm³ | Use 2.1 g/cm³ |
| Isosteric heat of adsorption (H₂) | 5 – 7 kJ/mol | Slightly higher than zeolite |
| Model structure | Amorphous carbon / slit-pore model | Use slit-pore geometry for GCMC |
| Effective pore width | 5 – 15 Å | Distributed; use 7 Å as mean |

## 2.4 Composite Bed Composition

| Parameter | Value |
| --- | --- |
| Zeolite mass fraction | 85 wt% (0.85) |
| Nano-AC mass fraction | 15 wt% (0.15) |
| Preparation method | Dry blending — assume intimate mechanical mixture |
| Total bed loading per run | ~90 g |
| Zeolite mass per run | 76.5 g |
| Nano-AC mass per run | 13.5 g |
| Composite treatment | No chemical bonding — physical mixture only |

# 3. Operating Conditions

These are the exact conditions under which the simulation must be run. These values are taken directly from the P&ID drawing PID-ZHS-FAB-002.

| Parameter | Value | Notes |
| --- | --- | --- |
| Simulation temperature | 195 K (−78 °C) | Dry-ice + acetone bath temperature. Fixed — do not vary. |
| Pressure range | 1, 3, 5, 7, 10 bar | Five discrete points. Simulate each separately. |
| Adsorbate molecule | Hydrogen (H₂) | 99.9% purity — treat as pure H₂ |
| Hydrogen model | Buch model or Darkrim-Levesque model | 2-site LJ model preferred for GCMC |
| Adsorption type | Physisorption only | No chemisorption — do NOT use reactive force fields |
| Equilibration type | Grand canonical (fixed μ, V, T) | For GCMC — chemical potential set by pressure |
| Vessel internal volume | 484 cm³ | π × (25mm)² × 250mm |
| Dead volume per end | 60 cm³ (30 cm³ × 2) | 30 mm space at each end cap |
| Active bed volume | ~364 cm³ | Vessel volume minus dead volumes |
| Void fraction (bed) | ~0.35 – 0.40 | Interparticle void; use 0.38 |
| Reporting units | wt% (g H₂ / 100 g adsorbent) | Standard gravimetric units |

## 3.1 Hydrogen Force Field Parameters

For GCMC simulation, the hydrogen molecule must be described by a force field. Use the Buch (1994) model as the first choice, or the Darkrim-Levesque (1998) model as the alternative. Both are freely available in the RASPA2 database.

| Model | σ (Å) | ε/k_B (K) | Bond length (Å) | Point charges |
| --- | --- | --- | --- | --- |
| Buch (1994) — RECOMMENDED | 2.96 | 34.2 | 0.74 (rigid) | None — non-polar model |
| Darkrim-Levesque (1998) | 2.958 | 36.7 | 0.74 (rigid) | ±0.468e on each site |

# 4. The Eight-Configuration Test Matrix

The simulation must be run for each of the following eight configurations. Each configuration is a unique combination of zeolite type, physical form, and composite status. The run numbers correspond exactly to those used in Chapter 3 and Chapter 4 of the thesis.

| Run | Zeolite | Physical Form | Nano-AC | Composite? | Priority |
| --- | --- | --- | --- | --- | --- |
| 1 | 13X | Granular | None | No (plain baseline) | HIGH |
| 2 | 13X | Powder | None | No (plain baseline) | HIGH |
| 3 | 5A | Granular | None | No (plain baseline) | MEDIUM |
| 4 | 5A | Powder | None | No (plain baseline) | MEDIUM |
| 5 | 13X | Granular | 15 wt% | YES | HIGH |
| 6 | 13X | Powder | 15 wt% | YES | HIGH |
| 7 | 5A | Granular | 15 wt% | YES | MEDIUM |
| 8 | 5A | Powder | 15 wt% | YES | MEDIUM |

NOTE: Run 6 (13X Powder + Nano-AC) is highlighted as the predicted best-performing configuration and should be validated first as a sanity check.

## 4.1 How to Model Each Configuration in Simulation

### Granular vs Powder Forms

In GCMC simulation using the crystal structure, both granular and powder configurations are modelled using the same unit cell — the crystal structure is identical. The difference between granular and powder is captured through a binder correction factor applied to the granular results:

- Granular result = GCMC output × (1 − binder_fraction) = GCMC output × 0.825

- Powder result = GCMC output × 1.0 (no binder correction)

- Additionally apply a powder kinetic enhancement of 1.15× to account for improved accessibility (from Erdogan et al., 2024)

### Composite (Zeolite + Nano-AC) Configurations

For composite runs (5–8), two approaches are available:

- Approach A (preferred): Run GCMC separately for the zeolite and for the nano-AC model. Combine results using a weighted average: n_composite = 0.85 × n_zeolite + 0.15 × n_carbon, then apply the synergistic enhancement factor of 1.40 from Hauli et al. (2025).

- Approach B (simpler): Apply the composite enhancement factor directly to the plain zeolite result: n_composite = 1.40 × n_zeolite (granular or powder as appropriate).

NOTE: Approach B is acceptable if time is limited. The 1.40× factor is literature-justified and the thesis will document this clearly.

# 5. Number of Simulation Runs Required

The table below summarises the total number of simulation runs required. Each 'run' here means one GCMC or ML simulation at a specific configuration and pressure point.

| Item | Count | Detail |
| --- | --- | --- |
| Material configurations | 8 | Runs 1–8 as defined in Section 4 |
| Pressure points per configuration | 5 | 1, 3, 5, 7, 10 bar |
| Base simulation runs | 40 | 8 × 5 = 40 individual isotherm points |
| Validation runs (77 K benchmark) | 10 | Plain 13X and 5A at 77 K, 5 pressures each |
| Sensitivity runs (optional) | 10 | Vary q_st between 4 and 8 kJ/mol for uncertainty analysis |
| **TOTAL MINIMUM** | **50** | 40 production + 10 validation |
| TOTAL WITH SENSITIVITY | 60 | 40 + 10 + 10 |

Run order recommendation: Complete the 10 validation runs at 77 K first and compare against Langmi et al. (2003) values before running the 195 K production simulations. If validation passes (within 15% of literature), proceed with production runs. If validation fails, the force field or structure requires adjustment before production results will be meaningful.

# 6. Validation Targets — What the Simulation Must Match

Before accepting any simulation results for use in the thesis, the simulator must verify that the model reproduces the following published experimental values within a tolerance of ±15%. These values are from Langmi et al. (2003) and represent the gold-standard benchmark for zeolite hydrogen storage.

Table 6.1: Validation targets — Langmi et al. (2003) at 77 K

| Pressure (bar) | Zeolite 13X target (wt%) | Zeolite 5A target (wt%) | Acceptable range 13X | Acceptable range 5A |
| --- | --- | --- | --- | --- |
| 1 | 0.48 | 0.32 | 0.41 – 0.55 | 0.27 – 0.37 |
| 3 | 0.87 | 0.58 | 0.74 – 1.00 | 0.49 – 0.67 |
| 5 | 1.12 | 0.74 | 0.95 – 1.29 | 0.63 – 0.85 |
| 7 | 1.28 | 0.85 | 1.09 – 1.47 | 0.72 – 0.98 |
| 10 | 1.42 | 0.94 | 1.21 – 1.63 | 0.80 – 1.08 |

NOTE: If the simulation output falls outside the acceptable range for more than 2 of the 5 pressure points for either zeolite, the simulation parameters must be reviewed before proceeding to 195 K production runs.

## 6.1 Temperature Correction Check

After validating at 77 K, apply the van 't Hoff correction to obtain expected values at 195 K using the formula:

n(195K) / n(77K)  =  exp[(q_st / R) × (1/195 − 1/77)]  ≈  0.0228   (for q_st = 4 kJ/mol)

The simulation output at 195 K should be approximately 2.28% of the 77 K value at each pressure point (for the same material). If the simulation produces values significantly different from this ratio, it indicates either a force field temperature-dependence issue or an error in the temperature setting.

# 7. Required Simulation Outputs

The following outputs must be delivered by the simulator for use in Chapter 4 of the thesis. All outputs must be provided in the formats specified.

## 7.1 Primary Output — Adsorption Isotherm Table

The main deliverable is a single master table in the following format (identical structure to Table 4.4 in the thesis Chapter 4 draft):

Required output format — master isotherm table

| Run | Configuration | 1 bar (wt%) | 3 bar (wt%) | 5 bar (wt%) | 7 bar (wt%) | 10 bar (wt%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 13X Granular (plain) | — | — | — | — | — |
| 2 | 13X Powder (plain) | — | — | — | — | — |
| 3 | 5A Granular (plain) | — | — | — | — | — |
| 4 | 5A Powder (plain) | — | — | — | — | — |
| 5 | 13X Granular + Nano-AC | — | — | — | — | — |
| 6 | 13X Powder + Nano-AC | — | — | — | — | — |
| 7 | 5A Granular + Nano-AC | — | — | — | — | — |
| 8 | 5A Powder + Nano-AC | — | — | — | — | — |

## 7.2 Additional Required Outputs

- Validation table: The simulated uptake values at 77 K for plain 13X and 5A, at all 5 pressure points, alongside the Langmi target values and the percentage error for each point.

- Isotherm plots: A single figure showing all 8 predicted isotherms on one graph (uptake in wt% on y-axis, pressure in bar on x-axis, each configuration as a separate line). PNG or SVG format, minimum 300 dpi.

- Force field / model parameters used: A brief summary (half a page) of exactly which force field, crystal structures, and simulation settings were used — required for the thesis methodology section.

- Convergence evidence: For GCMC, provide the production cycle count and a plot or table showing that uptake has converged (i.e. does not change with further cycles). This is required for academic credibility.

- Uncertainty estimate: For each configuration, an estimate of the simulation uncertainty (standard deviation across multiple runs or cycle blocks) expressed in wt%.

## 7.3 File Formats Required

| Deliverable | Format | Notes |
| --- | --- | --- |
| Master isotherm table | Excel (.xlsx) AND Word (.docx) | Both formats required |
| Isotherm plots | PNG (300 dpi minimum) | One combined figure, all 8 runs |
| Validation table | Excel (.xlsx) |  |
| Force field summary | Word (.docx) or PDF | Half to one page |
| Convergence evidence | Any readable format |  |
| Raw simulation output | Any format | For archive / reproducibility |

# 8. Crystal Structure Files and Where to Get Them

For GCMC simulation, the simulator requires crystallographic information files (.cif format) for the zeolite frameworks. These are freely available from the International Zeolite Association (IZA) Structure Database.

| Zeolite | Framework Code | Download URL | Notes |
| --- | --- | --- | --- |
| Zeolite 13X | FAU | iza-structure.org/databases/ | Download FAU.cif — use the Na-exchanged form |
| Zeolite 5A | LTA | iza-structure.org/databases/ | Download LTA.cif — modify cation to Ca²⁺/Na⁺ |
| Nano-AC | N/A — amorphous | Generate slit-pore model in RASPA or use carbon nanotube template | No CIF available — use model structure |

NOTE: The IZA structure files represent idealised crystalline frameworks. For a more realistic simulation, the extra-framework cation positions (Na⁺ for 13X, Ca²⁺/Na⁺ for 5A) must be placed correctly within the unit cell. RASPA2 has built-in support for common zeolite cation configurations.

# 9. Key Literature References for the Simulator

The simulator should be aware of the following references. These are the papers that establish the experimental baseline against which simulation results will be compared.

| Reference | What it provides | Relevance to simulation |
| --- | --- | --- |
| Langmi et al. (2003) J. Alloys Compd. 356–357, 710–715 | Baseline H₂ uptake for 13X and 5A at 77 K across 0–15 bar | PRIMARY VALIDATION TARGET — simulation must reproduce these values |
| Vitillo et al. (2005) J. Phys. Chem. B | Isosteric heats of adsorption 4–8 kJ/mol for zeolites | Sets the q_st parameter for force field and van 't Hoff correction |
| Bénard & Chahine (2007) Langmuir 23, 6905 | Thermodynamic limits of room-temperature physisorption | Contextualises the low uptake at 195 K |
| Erdogan et al. (2024) Int. J. Hydrogen Energy | FAU/MOR/MTW comparison + zeolite-carbon composites | Provides powder enhancement factor and composite behaviour data |
| Hauli et al. (2025) Chem. J. Moldova | Zeolite + activated charcoal composite — 30–50% enhancement | Source of the 1.40× composite enhancement factor |
| Akyalcin et al. (2024) Microporous Mesoporous Mater. | Acid-treated clinoptilolite, PVT method | Secondary validation reference |
| Buch (1994) / Darkrim-Levesque (1998) | H₂ force field parameters | Required for GCMC simulation setup |

# 10. Summary Checklist for the Simulator

Before delivering results, the simulator should confirm all of the following:

## Setup Checklist

- ✓  Crystal structure files (.cif) obtained for FAU (13X) and LTA (5A) from IZA database

- ✓  Hydrogen force field selected (Buch 1994 recommended)

- ✓  Zeolite force field selected (UFF or Dreiding for framework atoms)

- ✓  Extra-framework cations (Na⁺ for 13X, Ca²⁺/Na⁺ for 5A) correctly placed

- ✓  Temperature set to 195 K

- ✓  Pressure points: 1, 3, 5, 7, 10 bar

- ✓  Grand canonical ensemble (fixed μ, V, T) confirmed

## Validation Checklist (must complete before production runs)

- ✓  Validation runs at 77 K completed for plain 13X and 5A

- ✓  Simulated values at 77 K compared against Langmi et al. (2003) Table 6.1 targets

- ✓  All 10 validation points fall within ±15% of literature targets

- ✓  Temperature correction ratio checked: n(195K)/n(77K) ≈ 0.0228

## Production Run Checklist

- ✓  All 8 configurations simulated at all 5 pressure points = 40 runs total

- ✓  Binder correction applied to granular results (× 0.825)

- ✓  Powder enhancement applied to powder results (× 1.15)

- ✓  Composite enhancement applied to composite results (× 1.40)

- ✓  Convergence confirmed for each run

## Deliverables Checklist

- ✓  Master isotherm table (Excel + Word) — all 8 runs × 5 pressures

- ✓  Isotherm plots (PNG, 300 dpi, all 8 runs on one figure)

- ✓  Validation table with percentage errors vs Langmi targets

- ✓  Force field and model parameters summary (half page)

- ✓  Convergence evidence

- ✓  Uncertainty estimates per configuration

# 11. Expected Results Guide

The table below shows the values predicted by the analytical van 't Hoff correction method developed in Chapter 4. These are NOT targets — the simulation should produce its own values independently. However, if the simulation produces values dramatically different from these (more than a factor of 3), it is likely that a setup error has occurred and the simulator should review their inputs before delivering results.

Table 11.1: Chapter 4 analytical predictions at 195 K — for reference only, not targets

| Run | Configuration | 1 bar | 3 bar | 5 bar | 7 bar | 10 bar |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 13X Granular (plain) | 0.0110 | 0.0198 | 0.0255 | 0.0292 | 0.0324 |
| 2 | 13X Powder (plain) | 0.0127 | 0.0228 | 0.0293 | 0.0336 | 0.0373 |
| 3 | 5A Granular (plain) | 0.0073 | 0.0132 | 0.0169 | 0.0194 | 0.0214 |
| 4 | 5A Powder (plain) | 0.0084 | 0.0152 | 0.0194 | 0.0223 | 0.0246 |
| 5 | 13X Granular + Nano-AC | 0.0154 | 0.0277 | 0.0357 | 0.0409 | 0.0454 |
| 6 | 13X Powder + Nano-AC | 0.0177 | 0.0319 | 0.0411 | 0.0470 | 0.0522 |
| 7 | 5A Granular + Nano-AC | 0.0102 | 0.0185 | 0.0237 | 0.0272 | 0.0300 |
| 8 | 5A Powder + Nano-AC | 0.0117 | 0.0213 | 0.0273 | 0.0313 | 0.0345 |

NOTE: All values in wt% (grams H₂ per 100 grams adsorbent). Run 6 highlighted as the predicted best performer.

Questions or clarifications on this specification should be directed to Emmanuel Solomon-Eseh before simulation begins. Any changes to the material parameters, operating conditions, or configuration definitions must be agreed and documented before results are generated for thesis use.